# 125 MICRON CLEAR VELVET POLYCARBONATE

Description:  This is a clear velvet embossed polycarbonate film coated with a water clear acrylic pressure-sensitive adhesive and backed with an ultra smooth clear polyester release liner.

Application: An attractive film where optimum, clarity, dimensional stability and versatility in a protective over laminate are needed. Faceplates, nameplates and decorative trim parts are typical applications.

Physical Properties:

Film thickness:				125 micron + or – 10%

Adhesive:				Solvent Acrylic Permanent

Dimensional Stability:			Excellent

Abrasion Resistance:      		Excellent

Chemical Resistance:	Generally resistant to water, mild acids, salts & alkalis,                                                    petroleum based greases, oils and aliphatic solvents.

Minimum Application Temp:		+4 Deg C

Service Temperature:			-40 deg C to 130 deg C

The above specification is based on information obtained from the original manufacturer and is offered in good faith in accordance with the companies conditions to determine fitness for use.  No guarantee is offered or implied.  It is ultimate users’ responsibility to fully test the material and determine its suitability for the application intended.  Measurements and test results are nominal.   In accordance with a policy of continuous product improvement the manufacturer reserves the right to amend the specification without notice.