SUPER GLOSS CLEAR POLYESTER LAMINATE (PS0039)

Face:

Super Gloss Clear Polyester offers excellent optical clarity and dimensional stability with a good solvent.  Suitable to humidity temperature and is UV resistant.  Can be used for over-laminating on variable information labels, screen and digital printed images.

Thickness			75 micron +/-10%

Caliper				FTM 12

Adhesive:

It is a permanent ultra clear high performance acrylic adhesive which has an excellent adhesion on a broad range of materials and substrates.

Initial Tack			High

Final Adhesion		Very High

Min. App. Temp		+ 4ºC

Temp Range			-40ºC to +135ºC

UV Resistance 		Excellent

Chemical Resistance	3.5 - Good

Liner:

It is a clear polyester release liner ensuring adhesive smoothness.

Thickness		25 micron +/- 10%

The above specification is based on information obtained from the original manufacturer and is offered in good faith in accordance with the companies conditions to determine fitness for use.  No guarantee is offered or implied.  It is ultimate users’ responsibility to fully test the material and determine its suitability for the application intended.  Measurements and test results are nominal.   In accordance with a policy of continuous product improvement the manufacturer reserves the right to amend the specification without notice.