ULTRA DESTRUCTIBLE SATIN WHITE PVC 03 -126 (DIGITAL)

Face:

It is a 50µ Satin white destructible PVC with consistent satin gloss level and excellent printability via conventional inks.  It has been designed as a security film for tamper evidence on a broad range of substrates.  It has excellent UV, humidity and chemical resistance.

Thickness              50 micron

Adhesive:

It has a PAT1 high performance acrylic adhesive offers very good chemical, humidity and elevated temperature resistance.  It exhibits very good adhesion to a broad range of surfaces and is automotive approved.

Application Temp: 	+4 ºC

Service Temp:		-40ºC  to  +85 º C

Cohesive Strength	 Good

Initial Adhesion 	 1800 g/25mm

Adhesion after 48 Hrs	  2500+g/25mm

Backing:

It is a 11LLB is a 145gsm blue poly-coated Kraft release liner, selected for its lay flat and die cutting properties.

Outdoor durability:

5 years.  Destructible films are fragile and care should be taken.

This product is compliance under RoHS directive 2002/95/EC

The above specification is based on information obtained from the original manufacturer and is offered in good faith in accordance with the companies conditions to determine fitness for use.  No guarantee is offered or implied.  It is ultimate users’ responsibility to fully test the material and determine its suitability for the application intended.  Measurements and test results are nominal.   In accordance with a policy of continuous product improvement the manufacturer reserves the right to amend the specification without notice.