MATT SILVER VOID POLYESTER 02-268 (DIGITAL)

Face:

50µ Matt silver print receptive void polyester is designed as a security label stock that offers an instant VOID message upon removal of the converted label.  It’s consistent, smooth surface offers high resolution printing via conventional inks.

Thickness              	50 micron ± 10%

Chemical resistance 	Good

Adhesive:

P60 high Performance permanent acrylic adhesive, P60 exhibits very good chemical, humidity and UV resistance.  P60 offers excellent adhesion to most substrates combined with good low temperature adhesion.   Automotive approved.

Application Temp: 	+4 ºC

Service Temp:		-25ºC  to  +125º C

Cohesive Strength	 Good

Backing:

It has a 96gsm blue poly-coated glassine release liner.  The one side PE coated liner ensures adhesive smoothness.  It is suitable for high speed dispensing.

Application:

It is suitable for rating, warning, hazard, asset identification and serial numbered bar code labels.

Life Span:

Outdoor durability: 2 years.

This product is compliance under RoHS directive 2002/95/EC.

The above specification is based on information obtained from the original manufacturer and is offered in good faith in accordance with the companies conditions to determine fitness for use.  No guarantee is offered or implied.  It is ultimate users’ responsibility to fully test the material and determine its suitability for the application intended.  Measurements and test results are nominal.   In accordance with a policy of continuous product improvement the manufacturer reserves the right to amend the specification without notice.