# 3M GLOSS PLATINUM SILVER 7872 PET 50Mµ 350E

Face:

Gloss silver polyester, top coated for improved ink receptivity and designed for thermal transfer printing.  It is printable by all standard methods including flexography, hot foil, letterpress and screen process.  Typical applications include nameplates for durable electronic and sporting goods, property identification and asset labelling in harsh environments.

Thickness              50 micron ±5%

Basic weight

Adhesive:

A permanent modified acrylic aqueous dispersion which offers excellent adhesion even on textured surfaces as well as providing excellent temperature and chemical resistance.

Initial Tack            High

Final Adhesion      Very High

Min. App. Temp    +10ºC

Temp Range         -40ºC to +150ºC

UV Resistance

UL and cUL approved  (File  Number MH18072)

Conversion Advice:  Rotary die cutting is recommended.  Fanfolding of labels in not recommended.  Small labels should be evaluated carefully.  Winding tensions should be kept at a minimum to help prevent the adhesive from oozing.

Liner:

A white glassine liner double sided.

Thickness              56 micron ±5%

Basic Weight         65 gsm  ±5%

Shelf Life:

2 years when stored at 22ºC / 50% RH

The above specification is based on information obtained from the original manufacturer and is offered in good faith in accordance with the companies conditions to determine fitness for use.  No guarantee is offered or implied.  It is ultimate users’ responsibility to fully test the material and determine its suitability for the application intended.  Measurements and test results are nominal.   In accordance with a policy of continuous product improvement the manufacturer reserves the right to amend the specification without notice.