# ALUMINIUM METAL ASSET TAG

Face:

Anodised aluminium asset tags, perfect for testing and long-lasting applications. Available with adhesive or alternatively with drill holes for an even longer-life span and wider temperature range.

Product life: 					Decades in appropriate environments.

Thickness of base material:                 	1000 micron (1mm) ±10%.

Thickness & type of adhesive (if chosen):	110 micron ±10% permanent solvent acrylic (max. 120℃).

Temperature resistance (Ex. Adhesive)	12-hour cycle at 300℃ with no effect.

12-hour cycle at 500℃ saw bleaching within 2 minutes.

Abrasion resistance: 	Very high, no effect at all during 24000 cycles of a pighairbrush + water + talcum powder (1000gr. load); only slight dulling after 7000 cycles with a CS17 wheel (1000 gr. load).

Chemical resistance:	No effect at all when immersed in the following substances for 700 hrs: salt spray, mil-S-3136 hydrocarbon fluid, mil-S-5156 turbine + jet engine fuel, kerosene, skydroll, methyl ethylketone, ethyl acetate, xylol, heptane, ethyl alcohol.

Plus, no effect from the following: ferric chloride (10% solution for 24 hours), mil-P-21563 (soap solution for 16 hours), mil-C-25179 AI in heptane (25% solution, 1 min cleaning solution), sulphuric acid (10% solution for 24 hours), phosphoric acid (1% solution for 12 hours), nitric acid (3% solution for 72 hours), TSP (1% solution for 40 hours).

Slight dulling from ammonium hydroxide (10% solution 10 hours).