# MATT SILVER VOID PET

**Temp Range: -30ºC - +149ºC**

**Min. Application Temp: +4ºC**

**Face:**

A matt silver void polyester film with a selective release system for use in tamper evident labels. the coating gives excellent resistance to solvents, scuffing, moisture and ageing. Exceeding the face surface temperature may cause the void mechanism to fail.

**Thickness: 50 micron ±5%**

**Adhesive:**

A strong permanent acrylic adhesive with proven performance for standard labels, nameplates and other similar used. It has high cohesion and good resistance to heat, cold water and UV. It also has good quick-stick, peel and shear strength with excellent adhesion to low surface energy surfaces. It is designed for high speed automatic label application.

**Initial Tack**:  **Medium**

**Final Adhesion: High**

**Liner**

A polycoated glassine liner.

**Thickness: 74 micron ±5%**

**Basic Weight: 82 gsm**